## Slide 1
High Energy Lithium Carbon Monofluoride Batteries Qualified for Portable Power
Rob Gitzendanner, Greg Miller, Mario Destephen, Mark Robertson
This document does not contain technology or technical data controlled under either ITAR or EAR.

## Slide 2: EaglePicher at a Glance
30
Expertise in More than
Battery Chemistries
Small Business
Battery Manufacturing (335910)

## Slide 3: Battery Chemistries and Applications
Lithium-CFx
Lithium- Thionyl Chloride
Lithium-Oxyhalide
Lithium- Manganese Dioxide (MnO2)
Lithium- Thermal
BA5790
Thermal batteries
Primary (one-time use)
Aqueous (Ag-Zn, Alkaline)
Torpedoes
THAAD
Loitering Munitions
Conventional Lithium-Ion
Advanced
Lithium-Ion
(Silicon, High Energy)
Lithium Metal
Aqueous
(Ag-Zn)
UUVs
High Power Lithium-Ion
Military Aircraft
Satellites
Directed Energy
Space Exploration
UAS
Secondary (rechargeable)

## Slide 4: Hybrid CFx for Portable Soldier Power

## Slide 5: What is Hybrid/CFx
Hybrid of CFx and MnO2 chemistry to take advantage of both materials
High specific energy (>500Wh/kg) and energy density (>800 Wh/l)
Long shelf-life (>10 years), capacity loss <1%/year
Wide operating temperatures (-40°C to +85°C)

## Slide 6: Lithium Hybrid CFx Cells (Non-Rechargeable)
Enabling Characteristics
  Reduced heat generation vs. pure CFx
  Increased rate capability (up to 4C)
  Voltage drop is significantly reduced (vs CFx)
  Web coating process enables cylindrical and pouch cell formats
Applications
Monitoring
Soldier power
Space power
Strategic missiles
Unmanned aerial vehicles
Hybrid CFx D Cell
Hybrid CFx Pouch Cell
Comparable D-Size Cell | Li-SO2 | Li-MnO2 | Li-CFx (LCF-514) | Li-CFx/MnO2 (LCF-15004)
Operating Voltage (V) | 2.8 | 2.8 | 2.6 | 2.7
Capacity (Ah) | 7.5 | 13 | 20 | 16
Weight (g) | 85 | 122 | 72 | 96.5
Specific Energy (Wh/kg) | 247 | 298 | 710 | 448
Energy Density (Wh/L) | 382 | 662 | 1000 | 786

## Slide 7: Battery Specification
Battery produced is compliant with MIL-PRF-32271A, Performance Specification Batteries, Non-Rechargeable, Lithium General
  Type IV – Hybrid/CFx Battery
  Class 2 – Require complete discharge in order to be considered non-reactive for disposal, includes Complete Discharge Device (CDD)
  Features E – Battery contains: Short Circuit, Over Current, Over Temperature and Charge Protection, as well as State of Charge Indicator (SOCI) and State of Charge data output terminals
Recently completed all First Article Testing with approval from Government sponsor

## Slide 8: Battery Performance Testing – Capacity
~50% Greater run time with Hybrid/CFx battery
EaglePicher
Competitors Design

## Slide 9: Battery Performance Testing – Pulsed Power Test
Hybrid CFx battery provides ~50% greater run time.
EaglePicher
Competitors Design

## Slide 10: Low Temperature Performance
After exposure to high temp (55°C) and physical drop test, batteries soaked at -20°C and discharged.
Batteries exceed discharge requirement (7hrs) without significant temp rise on case.

## Slide 11: Batteries Transportation Testing
40 Cells and 8 Batteries have completed UN38.3 Testing
All tests Pass
Battery is UN3090 Class 9 Lithium Metal Battery, but otherwise unregulated for standard modes of transportation.

## Slide 12: Cell Impact Testing

## Slide 13: Forced Discharge

## Slide 14: Nail Penetration Testing

## Slide 15: Outside Testing - Complete
NSWC Crane – Safety
  Battery Voltage
  Constant Current Discharge & Reversal
  Short Circuit
  Charging
  Electrical Safety Device
DEVCOM C5ISR – Performance
  Visual/Mechanical
  Battery Voltage
  Desert Cycle Storage
  IT/ITP Capacity
  LT/LTP Capacity
  HT/HTP Capacity

## Slide 16: Production Ready
Semi-automated cell and battery production capability established and validated (MRL 10)
100% Domestic Cell and Battery Manufacturing

## Slide 17: Summary
Battery has completed all requirements for First Article testing IAW MIL-PRF-32271A
Transportation testing per UN38.3 complete
Safety assessment by NSWC Crane and Performance assessment by US Army C5ISR complete
Production line is established and proven capable
  All product and component drawings, materials specifications and documentation are released
  All manufacturing, inspection and test procedures released
  Material sources of supply have been identified and verified
High Energy, High Reliability, US Domestically Manufactured Energy Storage Solution Ready for the Warfighter.

## Slide 18
September 30-October 3, 2024
Glendalough Conference Center DoubleTree
Springfield, MO
Experience the Power
Keynote Speaker
John Kelly

## Slide 19
Thank You.