## Slide 1: Glatfelter Generation II Separator
DPEC Dave Rittenhouse
June 5, 2024

## Slide 3
GLATFELTER
AT A GLANCE
  16 Manufacturing Facilities: U.S. - Germany - Canada United Kingdom - France Philippines - Spain
  Founded in 1864
  Employees worldwide: 3,300
  Sales: $1.5 billion
Glatfelter Company Snapshot 2023
$
Notes: Update Numbers

## Slide 5: Old Hickory Advanced Battery Technology Center

## Slide 6: Nonwoven Web forming technologies used by Glatfelter
Inclined Wire-Wet laid Nonwovens
Air Laid
Spun lace-Hydroentangled
Largest capacity of Inclined wire machines-10
Largest producer of Airlaid materials

## Slide 7: Three Pillars of Glatfelter’s Electrical Business
Lead-Acid Batteries
Capacitors
Lithium-Ion Separators
Invested in DreamWeaver on 3-14-2014
Manufacturing Licensee
Wet laid paper making process
Fibers dispersed in water
Single layer, comprised of nano and micro fibers
Sought to advance separator technology
Kraft Capacitor Tissue
Aluminum Electrolytic Capacitors
Leading supplier of Pasting Paper world wide
Retention Mats for EFBs

## Slide 8: Objectives of Generation II Separator
Fast Charging Thin Safety Versatile Secure Economic | Increased charge rates without loss of capacity or cycle life Increased energy density, reduced weight/size Low thermal shrinkage with optional high-temperature variants Platform technology can readily be tuned to diverse applications US sourced technologies, materials and manufacture Margin compression impacting EV industry, savings needed

## Slide 9: Properties of Generation II vs. existing separators
Uniform highly tortuous fibrous structure
High porosity => high ionic conductivity
Through pore structure, no tortuosity of stretched films
Poor wicking properties

## Slide 10: Properties of Gen II vs Dry Process Separator
Property | Unit |  | GS12 | GS15 | GS22 | PP Dry Process
Nominal Thickness | μm |  | 12 | 15 | 22 | 25
Basis Weight | g/m² |  | 6 | 8 | 12 | -
Thermal Shrinkage (120°C for 1hr) | % | MD | 2% | 1% | 3% | 14%
 |  | TD | 2% | 2% | 2% | 0%
Air Permeability | mL/sec |  | 1,420 | 320 | 149 | 11
 | s/100mL |  | 6 | 9 | 16 | 200
Porosity | % |  | 54 | 58 | 59 | 55

## Slide 11: Wettability and Capillary Action
12 gsm Gen II after 1 minute
- ~0.25 ml of LiPF6 1M EC/DMC -
25um PP Dry Process after 1 minute
- ~0.25 ml of LiPF6 1M EC/DMC -

## Slide 12: Shrinkage Testing
~1% Shrinkage in TD and ~5% in MD
~2% Shrinkage in TD and ~28% in MD

## Slide 13: Cycle Life of Gen II vs. Dry Process Separator
Chart: Cycle C/3 at RT
Description | Ch. ID | # | Cycles | Capacity Ret.% | Loss/cycle % | Start Cap. | End. Cap. | DCIR
15um | 16-3-1 | 11 | 532 | 94.3 | 0.0107 | 1694.80 | 1598.40 | 65
22um | 16-2-3 | 21 | 508 | 93.5 | 0.0127 | 1710.20 | 1599.70 | 71
Celgard 2500 | 15-8-6 | 35 | 468 | 94.6 | 0.0115 | 1670.90 | 1581.20 | 61
Celgard 1611 | 15-7-2 | 28 | 467 | 93.2 | 0.0146 | 1695.60 | 1579.90 | 58

## Slide 14: Cycle Life of Gen II vs. Dry Process Separator
Chart: Cycle 1C at RT
Description | Ch. ID | # | Cycles | Capacity Ret.% | Loss/cycle | Start Cap. | End. Cap. | DCIR
15um | 16-5-3 | 9 | 756 | 92.5 | 0.01 | 1610 | 1489 | 62
22um | 16-2-1 | 19 | 749 | 89.4 | 0.0141 | 1695 | 1516 | 71
Celgard 2500 | 15-8-3 | 32 | 698 | 88.2 | 0.0168 | 1680 | 1483 | 61
Celgard 1611 | 15-7-1 | 27 | 698 | 90.4 | 0.0137 | 1693 | 1531 | 58
Changed from C/3 to 1C

## Slide 15: Cycle Life of Gen II vs. Dry Process Separator
Chart: Cycle 1C at 45°C
Description | Ch. ID | # | Cycles | Capacity Ret.% | Loss/cycle % | Start Cap. | End. Cap. | DCIR
15um | 86-3-6 | 7 | 755 | 94.3 | 0.0076 | 1652 | 1565 | 58
22um | - | - | - | - | - | - | - | -
Celgard 2500 | 86-4-5 | 31 | 699 | 90.9 | 0.013 | 1672 | 1520.00 | 65
Celgard 1611 | 86-3-5 | 26 | 694 | 83.5 | 0.0238 | 1701 | 1420.90 | 61

## Slide 16: Rate Capability vs. Dry Process Separator
Chart: Rate Capability
| C/3 | C/2 | C | 2C | 3C | C/3
Glatfelter 15um | 100 | 97.2393 | 92.5144 | 86.7011 | 81.5141 | 102.6817
Dry Process 16um | 100 | 97.8866 | 93.5821 | 87.6657 | 82.4776 | 101.1164
Chart: 30s Pulse Discharge
| C/2 | C | 2C | 4C | 8C | 12C | 16C
CG2075 | 4.134 | 4.076 | 3.964 | 3.775 | 3.417 | 3.033 | 2.492
15um | 4.138 | 4.088 | 3.997 | 3.83 | 3.519 | 3.141 | 2.351

## Slide 17: Developments
Working with different materials to increase safety for extreme temperature conditions.
Ability to use non-standard materials is beneficial for applications beyond typical lithium-ion battery applications.

## Slide 18: Developments
Adjustable pore size & porosity to match performance in end-use-
  Rate vs. Self-discharge
Surface functionalization to enable better wet out by organic electrolytes
  High viscosity FR electrolytes
  Reserve battery application requiring excellent wicking
Wet-out in aqueous electrolyte systems
Dendrite Suppression
  Electrochemical technology
  Nanoparticle technology for advanced lithium battery designs prone to dendrite formation, eg. Li-Metal
Coatings
  Extreme temperature resistance
  Adhesive layer
Extended Cell Life– HF Scaveging technology

## Slide 19: Commercial Status
Have been making highly reproducible separator for 3 years on semi-production equipment
Engagements with many customers
  MIL: High-Rate applications-UAVs, DEWs, & Safety-CWBs
  High-Energy materials, enables high charge & discharge rates, Si, Li-Metal
  Emerging chemistries: Zn, Al-Ion, Si, Li-Metal anodes
Have inventory of 12, 15, and 22 um for sampling.
Can quickly scale to full-scale production

## Slide 20: Business Strategy
Approaching battery market the same way that Glatfelter uses with its other businesses:
Closely engage with customers to understand their needs and tailor a solution to meet their needs.
We can produce sample-to-commercial quantities
The details of each project are unique

## Slide 21: Summary of Gen II Separator
High porosity enables fast charging & discharging (Achieving 4C rates).
  Currently determining max discharge capabilities in High power applications.
Cell performance is comparable to commercial high power dry process separator.
Base product stable to 120°C (vs. 90°C for stretched films).
  Higher temperature versions under development.
Platform versatility and robustness enabling:
  Thickness range of 12 =>175 u
  Compatibility with organic and aqueous electrolyte systems
  Extensive IP portfolio
U. S. based supply chain provides security and jobs, availability of developmental and scale-up quantities.
Platform offers economic advantages vs. available separators

## Slide 22: Thank you for your time.
Dave.Rittenhouse@Glatfelter.Com
404-372-5082